Supplementary material

Solid biofuel generation from Eucalyptus wood residues: An experimental comparison study of torrefaction, hydrothermal, and slow pyrolysis

Orlando Salcedo-Puertoa,*, Clara Mendoza-Martineza, Thiago de Paula Protásiob, Esa Vakkilainena

aLappeenranta-Lahti University of Technology LUT, Yliopistonkatu 34, FI-53850 Lappeenranta, Finland

bFederal University of Lavras (UFLA), Department of Forest Sciences, 37203-202, Lavras, MG, Brazil

Corresponding author at: School of Energy Systems, Lappeenranta-Lahti University of Technology LUT,  PL 20, 53851 Lappeenranta, Finland.

E-mail address: orlando.salcedo.puerto@outlook.com (O. Salcedo-Puerto). Tel. +358 0505285968

Contents

Additional information on i) Materials and methods, and ii) Results and Discussion

i) Additional Details on Materials and Methods.

Text S1. Experimental setups description

Torrefaction

Torrefaction was carried out in a vertical quartz glass tube, with a length of 780 mm and diameter of 45 mm, placed vertically inside a tube furnace (Figure 1a). To ensure an inert atmosphere during experiments, a continuous gas flow of nitrogen (0.5 L/min) was introduced at the bottom part of the reactor and maintained by Bronkhorst mass flow controllers during the experiments. Albeit torrefaction gas was filtered and cooled for analysis, this analysis is beyond the scope of this study. Temperature distribution was monitored by two thermocouples located above and below the grid. A PID controller was used to maintain the desired temperature inside the reactor during the selected time interval. For the torrefaction experiments, approximately 7 g of biomass was added to the reactor, and nitrogen gas purged the reactor for several minutes to remove oxygen from the system. The sample was then heated up to the desired temperature in the typical range of 200 °C to 300 °C at a residence time of 15 to 30 minutes at a heating rate of 2 ℃/min [1].

Hydrothermal carbonization

Hydrothermal carbonization was carried in a stainless-steel tube reactor (1 L inner volume and dimensions of 705 mm height and 42 mm inner diameter) using as heat source the same tube furnace as in torrefaction experiments (Figure 1b). The tube had a flange connection at the top part, and screw closing at the bottom. The unit was indirectly heated by a 10-kW electric heater coil and protected from heat losses by a thick insulation layer. Two type K thermocouples measured the internal temperatures at 245 mm and 645 mm from the top, while another thermocouple tracked the temperature on the outer surface of the reactor. A pressure sensor and a pressure relief valve were installed at the top of the unit. The desired temperature level inside the reactor during tests was maintained with a proportional-integral-derivative (PID) controller. To ensure an inert atmosphere during experiments, the reactor was purged with a gas flow of nitrogen (0.5 L/min) for several minutes.

In the HTC experiments, approximately 50 g of biomass was dispersed in 300 ml of water, stirred manually, and then loaded into the reactor. The sample was then heated up to the desired temperature in the range of 180 °C to 240 °C, at a heating rate of 2 ℃/min. In literature, the residence time varies from 30 min for non-lignocellulosic materials [2], to several hours for lignocellulosic biomass [3]. In this work, a residence time between 3 to 6 hours was chosen to ensure complete carbonization. After cooling to room temperature, the hydrochar and liquid product were collected and separated by vacuum filtration using a Büchner funnel with Whatman glass microfiber filter paper (grade GF/A). Hydrochar was subsequently dried overnight in an oven at a temperature of 105 ± 2 °C and kept in plastic bags for further analysis. All tests were performed in duplicates, and the average value was reported. Liquid and gaseous product analysis was ruled beyond the scope of the study.

Slow pyrolysis

A tubular reactor (Figure 1c) was used for the SP experiments. Approximately 350 g of EWR was used. The sample was inserted into a metal capsule with nominal dimensions of 30 cm in length and 12 cm in diameter. The carbonizations were carried out at final temperatures between 300 and 600 °C, typical operating ranges for this thermal conversion [4]. The heating rate was 2 °C/min in all experiments. To ensure an inert atmosphere during experiments, the reactor was purged with gas flow of nitrogen (0.5 l/min) for several minutes.

Text S2. Performance indicators

Solid mass yield (MY), energy densification factor (EDF), energy yield (EY), and fuel ratio (FR) were calculated through Eqs. (2)-(5), respectively:

| MY= mbpmf ×100% | (1) |
| --- | --- |
| EDF=HHVbpHHVf | (2) |
| EY=MY × EDF | (3) |
| FR= FCdbVMdb | (4) |

Where: mbp– by-product mass (d.b.) [g], mf– feedstock mass (d.b.) [g], HHVbp–higher heating value of by-product [MJ/kg] (d.b.), and HHVf–higher heating value feedstock [MJ/kg] (d.b.).

Text S3. Theoretical emission fractions equations

The EF of chemical pure carbon (EC), carbon monoxide (ECO), methane (ECH4), carbon dioxide (ECO2), and nitrogen oxides (ENOx) were determined using the following equations, Eqs. (6)-(10):

| Ec=C × uc | (5) |
| --- | --- |
| ECO=MMCO MMC×EC×CCO/C | (6) |
| ECH4=MMCH4 MMC×EC×CCH4/C | (7) |
| ECO2=MMCO2 MMC×(EC-MMCMMCO×ECO-MMcMMCH4×ECH4-26.431.4×ENMVOC | (8) |
| ENOx=MMNO2MMN×EC×NC×NNOx/N | (9) |

Where C and N are biomass’s carbon and nitrogen mass fractions. MMC, MMCO, MMCH4, MMCO2, and MMNO2 are the molar masses (g/mol). The dimensional factor uc= 0.88 is the portion of carbon oxidized during combustion. The portions of carbon emitted as CO and CH4 during combustion are expressed as CCO/C= 0.06 and CCH4/C= 0.005, respectively. NNOx/N= 0.122 is the part of nitrogen emitted as NOX in the combustion process. ENMVOC correspond to the emission factor of non-methane volatile organic compounds (VOCs) (0.009 for biomass).

ii) Additional material Results and discussion.
In this section are presented the results of solid fuels characterization (Table S1), combustion parameters and its comparison with literature data parameters (Table. S2), and the results corresponding to the ANOVA analyses (Table S3-S8)

Table S1. Experimental design CDD runs of two factors. a Temperature [°C] ;b TOR [min], HTC and SP [hour]; c dry basis; d calculated by [5]

| Run | Factors |  |  | Yields [%] |  |  | Proximate analysisc [%] |  |  |  |  | Atomic ratios |  |  | Calorific [MJ/kg] |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Temp.a | Timeb |  | MY | EY |  | VM | AC | FC | FR |  | O/C | H/C |  | HHV | SBCd |
| Raw Eucalyptus |  |  |  | - | - |  | 86.92 (0.49) | 0.31 (0.60) | 12.77 (0.16) | 0.15 (0.17) |  | 0.71 (0.11) | 1.70 (0.03) |  | 19.56 (0.11) | 20.48 (0.44) |
| Torrefaction |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1 | 200 | 15 |  | 91.16 (0.22) | 97.74 (0.00) |  | 84.52 (0.36) | 0.33 (0.31) | 15.15 (0.34) | 0.18 (0.19) |  | 0.58 (0.39) | 1.41 (0.49) |  | 20.98 (0.60) | 21.96 (0.59) |
| 2 | 300 | 15 |  | 77.55 (0.17) | 83.73 (0.01) |  | 79.55 (0.10) | 0.36 (0.00) | 20.09 (0.07) | 0.25 (0.00) |  | 0.56 (0.10) | 1.34 (0.05) |  | 21.12 (0.33) | 22.11 (0.25) |
| 3 | 200 | 30 |  | 90.45 (0.08) | 97.04 (0.37) |  | 85.45 (0.21) | 0.32 (0.00) | 14.23 (0.44) | 0.17 (0.03) |  | 0.59 (0.00) | 1.52 (0.14) |  | 20.99 (0.36) | 21.97 (0.19) |
| 4 | 300 | 30 |  | 75.23 (0.18) | 82.38 (0.03) |  | 79.02 (0.20) | 0.37 (0.10) | 20.60 (0.06) | 0.26 (0.49) |  | 0.54 (0.18) | 1.38 (0.01) |  | 21.42 (0.40) | 22.43 (0.00) |
| 5 | 179 | 22.5 |  | 92.69 (0.17) | 97.70 (0.14) |  | 85.13 (0.17) | 0.34 (0.25) | 14.54 (0.12) | 0.17 (0.31) |  | 0.65 (0.24) | 1.58 (0.21) |  | 20.62 (0.03) | 21.59 (0.16) |
| 6 | 320 | 22.5 |  | 73.25 (0.02) | 80.80 (0.22) |  | 78.92 (0.00) | 0.39 (0.39) | 20.69 (0.08) | 0.26 (0.17) |  | 0.51 (0.00) | 1.25 (0.22) |  | 21.58 (0.10) | 22.60 (0.43) |
| 7 | 250 | 12 |  | 87.70 (0.00) | 92.78 (0.14) |  | 81.80 (0.10) | 0.36 (0.15) | 17.84 (0.14) | 0.22 (0.00) |  | 0.56 (0.52) | 1.47 (0.03) |  | 20.70 (0.16) | 21.67 (0.02) |
| 8 | 250 | 33 |  | 83.35 (0.00) | 90.36 (0.40) |  | 80.87 (0.01) | 0.39 (0.60) | 18.74 (0.14) | 0.23 (0.13) |  | 0.55 (0.26) | 1.41 (0.00) |  | 21.21 (0.20) | 22.20 (0.00) |
| 9 | 250 | 22.5 |  | 86.12 (0.50) | 93.11 (0.17) |  | 81.06 (0.00) | 0.38 (0.14) | 18.56 (0.15) | 0.23 (0.24) |  | 0.56 (0.17) | 1.42 (0.28) |  | 21.15 (0.17) | 22.15 (0.06) |
| 10 | 250 | 22.5 |  | 85.13 (0.20) | 92.04 (0.34) |  | 81.06 (0.17) | 0.37 (0.08) | 18.56 (0.39) | 0.23 (0.45) |  | 0.56 (0.21) | 1.42 (0.17) |  | 21.15 (0.06) | 22.14 (0.45) |
| 11 | 250 | 22.5 |  | 84.13 (0.00) | 90.97 (0.18) |  | 81.06 (0.15) | 0.37 (0.00) | 18.56 (0.22) | 0.23 (0.13) |  | 0.56 (0.00) | 1.42 (0.20) |  | 21.16 (0.12) | 22.15 (0.42) |
| Hydrothermal carbonization |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1 | 180 | 3 |  | 72.34 (0.02) | 80.24 (0.20) |  | 73.14 (0.27) | 0.29 (0.40) | 26.57 (0.00) | 0.36 (0.13) |  | 0.52 (0.28) | 1.34 (0.54) |  | 21.70 (0.07) | 22.72 (0.48) |
| 2 | 240 | 3 |  | 51.63 (0.14) | 67.31 (0.18) |  | 46.71 (0.22) | 0.12 (0.19) | 53.16 (0.03) | 1.14 (0.15) |  | 0.34 (0.20) | 0.94 (0.00) |  | 25.51 (0.15) | 26.71 (0.19) |
| 3 | 180 | 6 |  | 69.52 (0.23) | 77.48 (0.09) |  | 61.14 (0.33) | 0.31 (0.57) | 38.55 (0.09) | 0.63 (0.05) |  | 0.47 (0.13) | 1.30 (0.23) |  | 21.80 (0.43) | 22.83 (0.07) |
| 4 | 240 | 6 |  | 47.10 (0.52) | 61.45 (0.46) |  | 47.04 (0.21) | 0.20 (0.23) | 52.76 (0.36) | 1.12 (0.56) |  | 0.33 (0.00) | 0.90 (0.18) |  | 25.52 (0.00) | 26.72 (0.12) |
| 5 | 168 | 4.5 |  | 73.89 (0.00) | 77.60 (0.06) |  | 77.84 (0.13) | 0.29 (0.53) | 21.87 (0.57) | 0.28 (0.00) |  | 0.57 (0.15) | 1.52 (0.00) |  | 20.54 (0.15) | 21.51 (0.01) |
| 6 | 252 | 4.5 |  | 50.56 (0.22) | 66.22 (0.00) |  | 45.09 (0.20) | 0.21 (0.00) | 54.70 (0.00) | 1.21 (0.21) |  | 0.29 (0.00) | 0.82 (0.00) |  | 25.62 (0.25) | 26.83 (0.30) |
| 7 | 210 | 2.5 |  | 67.21 (0.00) | 84.61 (0.32) |  | 55.32 (0.00) | 0.12 (0.09) | 44.56 (0.39) | 0.81 (0.55) |  | 0.45 (0.48) | 1.30 (0.00) |  | 24.63 (0.52) | 25.78 (0.07) |
| 8 | 210 | 6.5 |  | 56.89 (0.38) | 74.15 (0.53) |  | 54.84 (0.55) | 0.18 (0.10) | 44.98 (0.00) | 0.82 (0.22) |  | 0.40 (0.12) | 1.06 (0.17) |  | 25.50 (0.23) | 26.70 (0.51) |
| 9 | 210 | 4.5 |  | 59.71 (0.16) | 76.75 (0.16) |  | 55.96 (0.35) | 0.12 (0.06) | 43.92 (0.11) | 0.78 (0.49) |  | 0.45 (0.22) | 1.15 (0.01) |  | 25.15 (0.25) | 26.33 (0.21) |
| 10 | 210 | 4.5 |  | 59.05 (0.20) | 75.95 (0.14) |  | 55.05 (0.00) | 0.19 (0.35) | 44.76 (0.00) | 0.81 (0.43) |  | 0.44 (0.00) | 1.18 (0.15) |  | 25.16 (0.22) | 26.34 (0.06) |
| 11 | 210 | 4.5 |  | 59.59 (0.00) | 76.29 (0.24) |  | 55.90 (0.41) | 0.19 (0.05) | 43.91 (0.11) | 0.79 (0.00) |  | 0.43 (0.06) | 1.12 (0.18) |  | 25.05 (0.00) | 26.22 (0.23) |
| Slow pyrolysis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1 | 300 | 3.5 |  | 48.41 (0.27) | 67.25 (0.19) |  | 40.05 (0.19) | 0.46 (0.40) | 59.49 (0.12) | 1.49 (0.57) |  | 0.20 (0.00) | 0.68 (0.40) |  | 27.18 (0.00) | 28.45 (0.24) |
| 2 | 600 | 3.5 |  | 35.06 (0.00) | 58.25 (0.45) |  | 13.15 (0.05) | 0.37 (0.25) | 86.48 (0.48) | 6.58 (0.56) |  | 0.14 (0.13) | 0.55 (0.02) |  | 32.51 (0.10) | 34.03 (0.07) |
| 3 | 300 | 5.5 |  | 45.60 (0.07) | 66.91 (0.03) |  | 32.39 (0.28) | 0.41 (0.39) | 67.20 (0.00) | 2.07 (0.00) |  | 0.18 (0.05) | 0.64 (0.09) |  | 28.70 (0.00) | 30.05 (0.18) |
| 4 | 600 | 5.5 |  | 29.50 (0.21) | 48.78 (0.25) |  | 13.92 (0.12) | 0.40 (0.58) | 85.68 (0.24) | 6.16 (0.17) |  | 0.10 (0.14) | 0.34 (0.12) |  | 32.35 (0.19) | 33.87 (0.21) |
| 5 | 238 | 4.5 |  | 53.41 (0.33) | 71.59 (0.12) |  | 45.05 (0.12) | 0.37 (0.04) | 54.58 (0.15) | 1.21 (0.00) |  | 0.31 (0.04) | 0.91 (0.06) |  | 26.22 (0.00) | 27.46 (0.48) |
| 6 | 662 | 4.5 |  | 29.05 (0.13) | 47.85 (0.05) |  | 14.57 (0.17) | 0.40 (0.50) | 85.03 (0.56) | 5.84 (0.18) |  | 0.09 (0.23) | 0.23 (0.16) |  | 32.22 (0.54) | 33.73 (0.00) |
| 7 | 450 | 3 |  | 38.03 (0.28) | 59.87 (0.52) |  | 21.77 (0.02) | 0.40 (0.20) | 77.83 (0.14) | 3.58 (0.50) |  | 0.14 (0.49) | 0.57 (0.50) |  | 30.80 (0.17) | 32.25 (0.00) |
| 8 | 450 | 6 |  | 32.73 (0.57) | 53.10 (0.09) |  | 17.00 (0.10) | 0.40 (0.17) | 82.60 (0.06) | 4.86 (0.21) |  | 0.11 (0.25) | 0.51 (0.00) |  | 31.74 (0.20) | 33.23 (0.17) |
| 9 | 450 | 4.5 |  | 33.19 (0.06) | 53.48 (0.10) |  | 18.08 (0.46) | 0.40 (0.56) | 81.52 (0.24) | 4.51 (0.18) |  | 0.13 (0.25) | 0.41 (0.11) |  | 31.52 (0.06) | 33.01 (0.08) |
| 10 | 450 | 4.5 |  | 33.18 (0.07) | 53.44 (0.00) |  | 18.15 (0.00) | 0.40 (0.06) | 81.46 (0.12) | 4.49 (0.19) |  | 0.13 (0.18) | 0.43 (0.19) |  | 31.51 (0.17) | 32.99 (0.23) |
| 11 | 450 | 4.5 |  | 33.78 (0.12) | 54.43 (0.00) |  | 18.10 (0.10) | 0.40 (0.28) | 81.50 (0.13) | 4.50 (0.04) |  | 0.13 (0.23) | 0.41 (0.58) |  | 31.52 (0.19) | 33.00 (0.24) |

TGA Combustion parameters

Table S2. Thermal degradation characteristics of raw and treated Eucalyptus wood residues.

| Sample | TGAa | Tib | Tpb | Tbb | DTGmaxc | Ref |
| --- | --- | --- | --- | --- | --- | --- |
| Eucalyptus |  |  |  |  |  |  |
| E-raw | 20 | 250 | 336 | 617 | 21 | Study |
| E-raw | 20 | 524 | - | 387 | 5 | [6] |
| E-raw | 10 | 203 | 523 | 602 | - | [7] |
| E-raw | 5 | 243 | 327 | 499 | 12 | [8] |
| Torrefaction |  |  |  |  |  |  |
| TOR 300-30 | 20 | 305 | 330 | 628 | 22 | Study |
| TOR 300-30 | 20 | 339 | 451 | 574 | 3 | [6] |
| TOR 280-40 | 15 | 270 | 330 | 660 | - | [9] |
| TOR 250-30 | 20 | 262 | 319 | 489 | 5 | [6] |
| Hydrothermal carbonization |  |  |  |  |  |  |
| HTC 240-6 | 20 | 290 | 510 | 679 | 5 | Study |
| HTC 250-0.5 | 20 | 288 | 423 | 445 | - | [10] |
| HTC 220-1 | 5 | 275 | 321 | 532 | 10 | [8] |
| HTC 200-0.5 | 20 | 288 | 414 | 449 | - | [10] |
| Slow pyrolysis |  |  |  |  |  |  |
| SP 600-5.5 | 20 | 470 | 607 | 728 | 8 | Study |
| SP 630-20 | 2 | 390 | 445 | 495 | - | [11] |
| SP 550 | 20 | 250 | 360 | 450 | - | [12] |
| SP 450-0.5 | 10 | 332 | 474 | 488 | 16 | [13] |

a TGA heating rate; b T in °C; c DTG in %/min

ANOVA Analysis

Torrefaction experiments

Table S3. Anova result for the fitted (quadratic) model of response variables evaluated in torrefaction.

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| MY |  |  |  |  |  |  |
| Model | 415.56 | 5 | 83.11 | 80.11 | < 0.0001 | * |
| A. Temperature | 387.61 | 1 | 387.61 | 373.62 | < 0.0001 | * |
| B. Time | 10.78 | 1 | 10.78 | 10.39 | 0.0234 | * |
| AB | 0.0019 | 1 | 0.0019 | 0.0019 | 0.9672 |  |
| A² | 12.63 | 1 | 12.63 | 12.17 | 0.0175 | * |
| B² | 0.9837 | 1 | 0.9837 | 0.9482 | 0.3749 |  |
| Residual | 5.19 | 5 | 1.04 |  |  |  |
| Lack of Fit | 3.2 | 3 | 1.07 | 1.07 | 0.5159 |  |
| Pure Error | 1.99 | 2 | 0.9946 |  |  |  |
| Cor Total | 420.75 | 10 |  |  |  |  |
| R² | 0.9877 | Adjusted R² | 0.9753 | Predicted R² | 0.9353 |  |
| EY |  |  |  |  |  |  |
| Model | 361.23 | 5 | 72.25 | 65.64 | 0.0001 | * |
| A. Temperature | 345.64 | 1 | 345.64 | 314.03 | < 0.0001 | * |
| B. Time | 1.9 | 1 | 1.9 | 1.72 | 0.2461 |  |
| AB | 0.1174 | 1 | 0.1174 | 0.1067 | 0.7572 |  |
| A² | 12.78 | 1 | 12.78 | 11.61 | 0.0191 | * |
| B² | 0.039 | 1 | 0.039 | 0.0354 | 0.8581 |  |
| Residual | 5.5 | 5 | 1.1 |  |  |  |
| Lack of Fit | 3.22 | 3 | 1.07 | 0.9386 | 0.5529 |  |
| Pure Error | 2.29 | 2 | 1.14 |  |  |  |
| Cor Total | 366.74 | 10 |  |  |  |  |
| R² | 0.9850 | Adjusted R² | 0.97 | Predicted R² | 0.9236 |  |
| HHV |  |  |  |  |  |  |
| Model | 0.7625 | 5 | 0.1525 | 58.73 | 0.0002 | * |
| A. Temperature | 0.4008 | 1 | 0.4008 | 154.35 | < 0.0001 | * |
| B. Time | 0.2417 | 1 | 0.2417 | 93.09 | 0.0002 | * |
| AB | 0.001 | 1 | 0.001 | 0.4018 | 0.554 |  |
| A² | 0.0109 | 1 | 0.0109 | 4.19 | 0.0961 | * |
| B² | 0.0804 | 1 | 0.0804 | 30.95 | 0.0026 | * |
| Residual | 0.013 | 5 | 0.0026 |  |  |  |
| Lack of Fit | 0.013 | 3 | 0.0043 | 668.92 | 0.0015 | * |
| Pure Error | 0 | 2 | 0.000006463 |  |  |  |
| Cor Total | 0.7755 | 10 |  |  |  |  |
| R² | 0.9833 | Adjusted R² | 0.9665 | Predicted R² | 0.881 |  |
| VM |  |  |  |  |  |  |
| Model | 43.68 | 5 | 8.74 | 694.46 | < 0.0001 | * |
| A. Temperature | 41.31 | 1 | 41.31 | 3283.94 | < 0.0001 | * |
| B. Time | 1.05 | 1 | 1.05 | 83.36 | 0.0003 | * |
| AB | 0.0745 | 1 | 0.0745 | 5.92 | 0.0591 | * |
| A² | 1.25 | 1 | 1.25 | 99 | 0.0002 | * |
| B² | 0.0878 | 1 | 0.0878 | 6.98 | 0.0459 | * |
| Residual | 0.0629 | 5 | 0.0126 |  |  |  |
| Lack of Fit | 0.0629 | 3 | 0.021 | 7204.86 | 0.0001 | * |
| Pure Error | 0.00000582 | 2 | 0.00000291 |  |  |  |
| Cor Total | 43.75 | 10 |  |  |  |  |
| R² | 0.9986 | Adjusted R² | 0.9971 | Predicted R² | 0.9898 |  |
| FC |  |  |  |  |  |  |
| Model | 42.88 | 5 | 8.58 | 636.91 | < 0.0001 | * |
| A. Temperature | 40.6 | 1 | 40.6 | 3015.09 | < 0.0001 | * |
| B. Time | 1.02 | 1 | 1.02 | 75.66 | 0.0003 | * |
| AB | 0.078 | 1 | 0.078 | 5.79 | 0.0612 |  |
| A² | 1.18 | 1 | 1.18 | 87.92 | 0.0002 | * |
| B² | 0.0806 | 1 | 0.0806 | 5.98 | 0.0582 |  |
| Residual | 0.0673 | 5 | 0.0135 |  |  |  |
| Lack of Fit | 0.0673 | 3 | 0.0224 | 7422.4 | 0.0001 | * |
| Pure Error | 0.000006047 | 2 | 0.000003023 |  |  |  |
| Cor Total | 42.95 | 10 |  |  |  |  |
| R² | 0.9984 | Adjusted R² | 0.9969 | Predicted R² | 0.9889 |  |

Table S4. Regression coefficients for torrefaction response variables.

|  | Intercept | A | B | AB | A2 | B2 |
| --- | --- | --- | --- | --- | --- | --- |
| MY |  |  |  |  |  |  |
| Coefficient | 85.12 | -6.96 | -1.16 | -0.022 | -1.5 | 0.4174 |
| Stdr. Error | 0.5881 | 0.3601 | 0.3601 | 0.5093 | 0.4286 | 0.4286 |
| EY |  |  |  |  |  |  |
| Coefficient | 92.04 | -6.57 | -0.4871 | -0.1713 | -1.5 | -0.0831 |
| Stdr. Error | 0.6057 | 0.3709 | 0.3709 | 0.5246 | 0.4415 | 0.4415 |
| HHV |  |  |  |  |  |  |
| Coefficient | 21.15 | 0.2238 | 0.1738 | -0.0161 | 0.0439 | -0.1193 |
| Stdr. Error | 0.0294 | 0.018 | 0.018 | 0.0255 | 0.0214 | 0.0214 |
| VM |  |  |  |  |  |  |
| Coefficient | 81.06 | -2.27 | -0.3621 | 0.1365 | 0.4696 | 0.1247 |
| Stdr. Error | 0.0648 | 0.0397 | 0.0397 | 0.0561 | 0.0472 | 0.0472 |
| FC |  |  |  |  |  |  |
| Coefficient | 18.56 | 2.25 | 0.3569 | -0.1396 | -0.4579 | -0.1195 |
| Stdr. Error | 0.067 | 0.041 | 0.041 | 0.058 | 0.0488 | 0.0488 |

Hydrothermal carbonization experiments

Table S5. Anova result for the fitted (quadratic) model of response variables evaluated in hydrothermal carbonization.

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| MY |  |  |  |  |  |  |
| Model | 791.62 | 5 | 158.32 | 28.72 | 0.0011 | * |
| A. Temperature | 724.38 | 1 | 724.38 | 131.42 | < 0.0001 | * |
| B. Time | 60.23 | 1 | 60.23 | 10.93 | 0.0213 | * |
| AB | 0.7216 | 1 | 0.7216 | 0.1309 | 0.7323 |  |
| A² | 4.48 | 1 | 4.48 | 0.8135 | 0.4084 |  |
| B² | 3.63 | 1 | 3.63 | 0.6587 | 0.4539 |  |
| Residual | 27.56 | 5 | 5.51 |  |  |  |
| Lack of Fit | 27.32 | 3 | 9.11 | 75.52 | 0.0131 | * |
| Pure Error | 0.2412 | 2 | 0.1206 |  |  |  |
| Cor Total | 819.18 | 10 |  |  |  |  |
| R² | 0.9664 | Adjusted R² | 0.9327 | Predicted R² | 0.7622 |  |
| EY |  |  |  |  |  |  |
| Model | 396.22 | 5 | 79.24 | 6.82 | 0.0275 | * |
| A. Temperature | 253.66 | 1 | 253.66 | 21.84 | 0.0055 | * |
| B. Time | 68.48 | 1 | 68.48 | 5.89 | 0.0595 |  |
| AB | 2.4 | 1 | 2.4 | 0.2067 | 0.6684 |  |
| A² | 58.39 | 1 | 58.39 | 5.03 | 0.075 |  |
| B² | 1.53 | 1 | 1.53 | 0.1317 | 0.7315 |  |
| Residual | 58.08 | 5 | 11.62 |  |  |  |
| Lack of Fit | 57.77 | 3 | 19.26 | 120.63 | 0.0082 | * |
| Pure Error | 0.3192 | 2 | 0.1596 |  |  |  |
| Cor Total | 454.31 | 10 |  |  |  |  |
| R² | 0.8721 | Adjusted R² | 0.7443 | Predicted R² | 0.6364 |  |
| HHV |  |  |  |  |  |  |
| Model | 34.68 | 5 | 6.94 | 61.47 | 0.0002 | * |
| A. Temperature | 27.04 | 1 | 27.04 | 239.62 | < 0.0001 | * |
| B. Time | 0.2304 | 1 | 0.2304 | 2.04 | 0.2124 |  |
| AB | 0.002 | 1 | 0.002 | 0.0174 | 0.9002 |  |
| A² | 7.18 | 1 | 7.18 | 63.61 | 0.0005 |  |
| B² | 0.1056 | 1 | 0.1056 | 0.9356 | 0.3778 |  |
| Residual | 0.5642 | 5 | 0.1128 |  |  |  |
| Lack of Fit | 0.5563 | 3 | 0.1854 | 47.01 | 0.0209 | * |
| Pure Error | 0.0079 | 2 | 0.0039 |  |  |  |
| Cor Total | 35.25 | 10 |  |  |  |  |
| R² | 0.984 | Adjusted R² | 0.968 | Predicted R² | 0.8873 |  |
| VM |  |  |  |  |  |  |
| Model | 1049.37 | 5 | 209.87 | 45.65 | 0.0004 | * |
| A. Temperature | 942.74 | 1 | 942.74 | 205.05 | < 0.0001 | * |
| B. Time | 19.08 | 1 | 19.08 | 4.15 | 0.0972 |  |
| AB | 38.01 | 1 | 38.01 | 8.27 | 0.0348 |  |
| A² | 38.16 | 1 | 38.16 | 8.3 | 0.0345 |  |
| B² | 1.98 | 1 | 1.98 | 0.4302 | 0.5409 |  |
| Residual | 22.99 | 5 | 4.6 |  |  |  |
| Lack of Fit | 22.47 | 3 | 7.49 | 28.85 | 0.0337 | * |
| Pure Error | 0.5192 | 2 | 0.2596 |  |  |  |
| Cor Total | 1072.36 | 10 |  |  |  |  |
| R² | 0.9786 | Adjusted R² | 0.9571 | Predicted R² | 0.8499 |  |
| FC |  |  |  |  |  |  |
| Model | 1059.27 | 5 | 211.85 | 46.97 | 0.0003 | * |
| A. Temperature | 951.12 | 1 | 951.12 | 210.89 | < 0.0001 | * |
| B. Time | 18.51 | 1 | 18.51 | 4.1 | 0.0986 | * |
| AB | 38.35 | 1 | 38.35 | 8.5 | 0.0332 | * |
| A² | 39.64 | 1 | 39.64 | 8.79 | 0.0314 | * |
| B² | 1.99 | 1 | 1.99 | 0.4421 | 0.5355 |  |
| Residual | 22.55 | 5 | 4.51 |  |  |  |
| Lack of Fit | 22.07 | 3 | 7.36 | 30.87 | 0.0315 | * |
| Pure Error | 0.4767 | 2 | 0.2384 |  |  |  |
| Cor Total | 1081.82 | 10 |  |  |  |  |
| R² | 0.9792 | Adjusted R² | 0.9583 | Predicted R² | 0.8539 |  |

Table S6. Regression coefficients for hydrothermal carbonization response variables.

|  | Intercept | A | B | AB | A2 | B2 |
| --- | --- | --- | --- | --- | --- | --- |
| MY |  |  |  |  |  |  |
| Coefficient | 59.45 | -9.52 | -2.74 | -0.4247 | 0.8911 | 0.8018 |
| Stdr. Error | 1.36 | 0.8301 | 0.8301 | 1.17 | 0.988 | 0.988 |
| EY |  |  |  |  |  |  |
| Coefficient | 76.33 | -5.63 | -2.93 | -0.7747 | -3.22 | 0.5205 |
| Stdr. Error | 1.97 | 1.21 | 1.21 | 1.7 | 1.43 | 1.43 |
| HHV |  |  |  |  |  |  |
| Coefficient | 25.12 | 1.84 | 0.1697 | -0.0222 | -1.13 | -0.1367 |
| Stdr. Error | 0.1939 | 0.1188 | 0.1188 | 0.168 | 0.1414 | 0.1414 |
| VM |  |  |  |  |  |  |
| Coefficient | 55.63 | -10.86 | -1.54 | 3.08 | 2.6 | -0.5918 |
| Stdr. Error | 1.24 | 0.7581 | 0.7581 | 1.07 | 0.9023 | 0.9023 |
| FC |  |  |  |  |  |  |
| Coefficient | 44.2 | 10.9 | 1.52 | -3.1 | -2.65 | 0.5942 |
| Stdr. Error | 1.23 | 0.7508 | 0.7508 | 1.06 | 0.8937 | 0.8937 |

Slow pyrolysis experiments

Table S7. Anova result for the fitted (quadratic) model of response variables evaluated in slow pyrolysis.

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| MY |  |  |  |  |  |  |
| Model | 646.07 | 5 | 129.21 | 91.99 | < 0.0001 | * |
| A. Temperature | 510.29 | 1 | 510.29 | 363.27 | < 0.0001 | * |
| B. Time | 31.43 | 1 | 31.43 | 22.37 | 0.0052 | * |
| AB | 1.89 | 1 | 1.89 | 1.35 | 0.2982 |  |
| A² | 102.42 | 1 | 102.42 | 72.91 | 0.0004 | * |
| B² | 10.04 | 1 | 10.04 | 7.15 | 0.0442 | * |
| Residual | 7.02 | 5 | 1.4 |  |  |  |
| Lack of Fit | 6.78 | 3 | 2.26 | 18.7 | 0.0512 |  |
| Pure Error | 0.2418 | 2 | 0.1209 |  |  |  |
| Cor Total | 653.09 | 10 |  |  |  |  |
| R² | 0.9892 | Adjusted R² | 0.9785 | Predicted R² | 0.9253 |  |
| EY |  |  |  |  |  |  |
| Model | 602.89 | 5 | 120.58 | 38.96 | 0.0005 | * |
| A. Temperature | 460.62 | 1 | 460.62 | 148.85 | < 0.0001 | * |
| B. Time | 46.99 | 1 | 46.99 | 15.19 | 0.0114 | * |
| AB | 20.87 | 1 | 20.87 | 6.74 | 0.0484 | * |
| A² | 69.79 | 1 | 69.79 | 22.55 | 0.0051 | * |
| B² | 20.36 | 1 | 20.36 | 6.58 | 0.0503 |  |
| Residual | 15.47 | 5 | 3.09 |  |  |  |
| Lack of Fit | 14.84 | 3 | 4.95 | 15.57 | 0.061 |  |
| Pure Error | 0.6353 | 2 | 0.3176 |  |  |  |
| Cor Total | 618.37 | 10 |  |  |  |  |
| R² | 0.975 | Adjusted R² | 0.95 | Predicted R² | 0.8271 |  |
| HHV |  |  |  |  |  |  |
| Model | 47.6 | 5 | 9.52 | 1205.49 | < 0.0001 | * |
| A. Temperature | 38.06 | 1 | 38.06 | 4819.5 | < 0.0001 | * |
| B. Time | 0.9075 | 1 | 0.9075 | 114.91 | 0.0001 | * |
| AB | 0.7114 | 1 | 0.7114 | 90.08 | 0.0002 | * |
| A² | 7.67 | 1 | 7.67 | 971.09 | < 0.0001 | * |
| B² | 0.1123 | 1 | 0.1123 | 14.23 | 0.013 | * |
| Residual | 0.0395 | 5 | 0.0079 |  |  |  |
| Lack of Fit | 0.0394 | 3 | 0.0131 | 333.81 | 0.0234 |  |
| Pure Error | 0.0001 | 2 | 0 |  |  |  |
| Cor Total | 47.64 | 10 |  |  |  |  |
| R² | 0.9992 | Adjusted R² | 0.9983 | Predicted R² | 0.9941 |  |
| VM |  |  |  |  |  |  |
| Model | 1223.86 | 5 | 244.77 | 1518.4 | < 0.0001 | * |
| A. Temperature | 978.37 | 1 | 978.37 | 6069.09 | < 0.0001 | * |
| B. Time | 23.25 | 1 | 23.25 | 144.2 | < 0.0001 | * |
| AB | 17.75 | 1 | 17.75 | 110.12 | 0.0001 | * |
| A² | 197.88 | 1 | 197.88 | 1227.51 | < 0.0001 | * |
| B² | 2.82 | 1 | 2.82 | 17.47 | 0.0087 | * |
| Residual | 0.806 | 5 | 0.1612 |  |  |  |
| Lack of Fit | 0.804 | 3 | 0.268 | 264.26 | 0.0338 |  |
| Pure Error | 0.002 | 2 | 0.001 |  |  |  |
| Cor Total | 1224.67 | 10 |  |  |  |  |
| R² | 0.9993 | Adjusted R² | 0.9987 | Predicted R² | 0.9953 |  |
| FC |  |  |  |  |  |  |
| Model | 1225.43 | 5 | 245.09 | 1333.9 | < 0.0001 | * |
| A. Temperature | 979.74 | 1 | 979.74 | 5332.34 | < 0.0001 | * |
| B. Time | 23.32 | 1 | 23.32 | 126.94 | < 0.0001 | * |
| AB | 18.07 | 1 | 18.07 | 98.34 | 0.0002 | * |
| A² | 197.75 | 1 | 197.75 | 1076.27 | < 0.0001 | * |
| B² | 2.86 | 1 | 2.86 | 15.56 | 0.0109 | * |
| Residual | 0.9187 | 5 | 0.1837 |  |  |  |
| Lack of Fit | 0.9167 | 3 | 0.3056 | 301.29 | 0.0343 |  |
| Pure Error | 0.002 | 2 | 0.001 |  |  |  |
| Cor Total | 1226.35 | 10 |  |  |  |  |
| R² | 0.9993 | Adjusted R² | 0.9985 | Predicted R² | 0.9947 |  |

Table S8. Regression coefficients for slow pyrolysis response variables.

|  | Intercept | A | B | AB | A2 | B2 |
| --- | --- | --- | --- | --- | --- | --- |
| MY |  |  |  |  |  |  |
| Coefficient | 33.38 | -7.99 | -1.98 | -0.6877 | 4.26 | 1.33 |
| Stdr. Error | 0.6843 | 0.419 | 0.419 | 0.5926 | 0.4987 | 0.4987 |
| EY |  |  |  |  |  |  |
| Coefficient | 53.78 | -7.59 | -2.42 | -2.28 | 3.52 | 1.9 |
| Stdr. Error | 1.02 | 0.6219 | 0.6219 | 0.8796 | 0.7403 | 0.7403 |
| HHV |  |  |  |  |  |  |
| Coefficient | 31.52 | 2.18 | 0.3368 | -0.4217 | -1.17 | -0.141 |
| Stdr. Error | 0.0513 | 0.0314 | 0.0314 | 0.0444 | 0.0374 | 0.0374 |
| VM |  |  |  |  |  |  |
| Coefficient | 18.11 | -11.06 | -1.7 | 2.11 | 5.92 | 0.7061 |
| Stdr. Error | 0.2318 | 0.142 | 0.142 | 0.2008 | 0.169 | 0.169 |
| FC |  |  |  |  |  |  |
| Coefficient | 81.49 | 11.07 | 1.71 | -2.13 | -5.92 | -0.7116 |
| Stdr. Error | 0.2475 | 0.1515 | 0.1515 | 0.2143 | 0.1804 | 0.1804 |